MAGNORM: A PROGRAM FOR THE STUDY OF MAGNESIA REFRACTORIES.

G. Tsambourakis

Division of Mineral Products, CSIRO, Port Melbourne, Victoria, Australia.

Dead-burned magnesia is one of the major raw materials used in the manufacture of refractories that do not melt below 2500oC.

The MgO content is, in itself, not the only factor that is industrially important. Impurity levels are equally important and can affect the slag resistance and high melting point properties of the product due to the formation of low melting phases such as monticellite (CMS, CaMgSiO4,or CaO MgO SiO2), merwinite (C3MS2, Ca3Mg(SiO4)2 or 3CaO MgO 2SiO2) and bredigite (C7MS4, Ca7Mg(SiO4)4 or CaO MgO 4SiO2).  The presence and proportion of these phases is critical, but, chemical analysis cannot presently yield such information.

CSIRO Division of Mineral Products researchers use the Rietveld method of phase analysis to determine the abundance of individual phase components of various materials, including magnesia refractories1-3. However, for magnesia refractories, the accuracy of the Rietveld results has not yet been tested against an alternative method.  The determination of phase abundances by point counting techniques is a very difficult if not impossible task. A procedure for calculating the phase compositions from chemical data - such as the Bogue method used in cement industry4 - has not so far been developed.  This article describes such a method.

Methodology

MAGNORM, similar to all other existing norms, converts analytical data into a standard set of hypothetical phases.  The calculations are based on the following assumptions;

* The analysed material is fresh and representative of the bulk sample;

* All oxides required for the calculations were accurately analysed;

* the composition of the phases actually present in the studied material is not considerably different from that calculated by the norm (MAGNORM uses standard idealised stoichiometric compositions);

* The SiO2 phases-such as quartz, tridymite, cristobalite-would not survive at the temperatures used for refractory production;

* Neither glass nor composition zoning are present;

* Chromite is the only chromium containing phase;

* Calcium zirconate is the only zirconium containing compound;

* Brucite is the only hydrated phase present (theoretically, freshly made refractories do not contain hydrated phases).

The program does not calculate portlandite.

MAGNORM first calculates the calcium to silica ratio (CSR) and the iron to calcium ratio (ICR).  It then continues with the calculation of brucite (Mg(OH)2 or MgO.H2O) (using the water content), chromite (using the Cr2O3 content) and calcium zirconate (using the ZrO2 content).

There are special instructions, based on combinations of the two parameters (CSR and ICR) and/or the presence of calcium zirconate or chromite.

The calculation of the normative phases continues using one of two available paths.  One path follows the special instructions, and calculates specific minerals directly.  For example; if calcium zirconate is present, MAGNORM proceeds with the calculation of bredigite.

The alternative path is used when none of the special conditions apply.  In this path, MAGNORM calculates phases by eliminating the SiO2 amount first, followed by the CaO amount.  This is achieved by following a procedure that commences with the calculation of dicalcium silicate (C2S, Ca2SiO4 or 2CaO.SiO2) and continues until there is no SiO2 remains. When, at various stages, SiO2 remains unused (i.e, is in excess) because of lack of CaO, MAGNORM restarts, using in the second attempt phases that contain less CaO, some MgO and more SiO2.  This process continues until there are no further improvements possible.  Any excess amount of CaO is then presented as lime (Lm, CaO) and any excess amount of SiO2 is presented as silica (Si).

Chemical Analysis

MAGNORM is calculated entirely from the analytical data because the main interest is to create compatible results between samples.

The oxides required for the calculations are: SiO2, Al2O3, Fe2O3, MnO, MgO, CaO, Cr2O3, ZrO2 and H2O+.  These oxides, except Cr2O3 and ZrO2, are included in most standard analytical routines.

Magnesia refractories are often doped with chromium or zirconia in order to improve their physical properties. Therefore, both Cr2O3 and ZrO2 should be included in the analytical routine.

Boron (B2O3), an important but very minor impurity, is not included in the calculations because most chemical analyses do not include B2O3, and the phases that incorporate B2O3 are unknown.

The amount of water present is used to calculate brucite. Therefore, it should be determined on the freshest possible sample and on a dry basis.  The following procedure is adequate; heat the sample at 120oC for 120 minutes to remove the hygroscopic moisture; re-weighed the sample to establish its weight on a dry basis and heat it at 1100oC for at least 12 hours to determine the water loss.

MAGNORM Phases Calculated

The periclase (Per, MgO), brucite (Bru), lime (Lm), dicalcium silicate (C2S), monticellite (CMS), merwinite (C3MS2), bredigite (C7MS4), chromite (Cm), calcium zirconate (Cz) and silica (Si) are included in the calculations.  These phases were identified in the X-ray diffraction patterns of 29 test samples obtained from refractory manufacturers around the world.

The presence of unexpected phases (such as brucite, bredigite and chromite which indicates disequilibrium), the absence of forsterite when SiO2 is in excess and problems associated with the calculation of dicalcium silicate (C2S) and tricalcium silicate (C3S) as separate phases when present together, made phase diagrams useful only as a guide.

Periclase is a dominant phase in high purity magnesia refractories.  It has the highest melting point of all magnesium phases (2800oC).

Freshly made refractories should not contain hydrated minerals such as brucite because it decomposes above 550oC. however, when they are exposed to the atmosphere, magnesia refractories absorb moisture and brucite forms from periclase.  Because hydration can occur at room temperature, it is important to analyse and determine water on freshly made refractory samples.

Lime is a relatively rare but desirable phase because of its high melting point (2570oC).  If CaO remains in excess, it is presented as lime (Lm).  Lime, can hydrate and form portlandite Ca(OH)2.  MAGNORM, in its present form, does not calculate portlandite because portlandite is rare.

Dicalcium silicate is a phase with a high melting point (2130oC.), making it another desirable phase.  There are four polymorphic modifications of this phase5 that cannot be calculated individually.  MAGNORM calculates and presents as dicalcium silicate all C2S modifications.  Furthermore, MAGNORM in its present form does not calculate alite (C3S) as a separate phase.  If alite is present, its abundance is incorporated in the dicalcium silicate amount by default.  Corrections are difficult to make and were not considered mainly because magnesia refractories contain small amounts of alite, if any, and the error is negligible.

Monticellite is an undesirable phase because of its low melting point (1500oC).  The Ca:Mg ratio is 1:1.

Merwinite is another undesirable phase because of its low melting point (1575oC).  Merwinite is a dicalcium silicate in terms of composition, with one fourth of the two Ca atoms replaced by one Mg atom (Ca:Mg ratio 3:1).  Small amounts of alumina and iron can be present in this phase.

Bredigite is also an undesirable phase.  It exists in nature and decomposes above 1375oC to form dicalcium silicate and merwinite. Bredigite is unstable bellow 980oC.  Theoretically, bredigite should not be present in magnesia refractories because it would not survive at the high temperatures used for the refractory production. However, it has been identified in X-ray diffraction patterns in all zirconia doped samples and there must be a good reason.

Magnesia refractories can be doped with zirconia to improve bonding, minimise slag attack, and increase high temperature strength.  XRD patterns have shown that calcium zirconate (CaZrO3 or CaO ZrO2) is the phase formed. Therefore, MAGNORM calculates calcium zirconate in samples that contain ZrO2.

Cr2O3 is also used for doping magnesia refractories in order to improve their physical properties.  In this case, based entirely on x-ray results obtained for a range of refractories, chromite and not a magnesium-iron-spinel is the phase calculated in samples that contain Cr2O3.

In some rare cases, small amounts of silica remain unused in the calculations and these are presented as excess silica (Si).  This does not mean that SiO2 is actually present as a phase, but it rather indicates that the hypothetical composition of one or more calculated phases differ from that of the real phases in the sample.  With a melting point of 1710oC (high cristobalite), SiO2 would not survive at the temperatures used for refractory production.

Discussion of Results

Unlike the mode, which expresses the weight percentages of the phases actually present, the MAGNORM converts analytical data of magnesia refractories, expressed as oxides, as a standard set of hypothetical phases.  This hypothetical composition is unlikely to match the mode. Therefore, norm and mode compositions can differ widely.  The main interest in the MAGNORM is to create results that are credible and usefully comparable.

Twenty-nine magnesia refractory bricks were used for this study.  These samples were part of an earlier characterisation study of magnesia refractories. They had been chemically analysed (bulk) and their phase abundances determined using Rietveld analysis of XRD data.  The MAGNORM results, calculated using the bulk analysis data, were compared with the phase abundances (mode) as determined by the RIETVELD method.

Originally, the samples were not analysed for ZrO2 and Cr2O3, and the water was not measured on a dry basis.  Reanalysing the samples was not possible because the samples were stored for many years and were altered.  Therefore the ZrO2, Cr2O3 and H2O values used in MAGNORM calculations were derived from the (equivalent) phase abundances determined by Rietveld refinement.  Because there are no further samples currently available, improvements are not yet possible.

The MAGNORM results compare favourably with corresponding Rietveld modes. The studied samples were separated into groups according to their phase compositions.

The following provide a better understanding of the results:

* MAGNORM's figures for the phase periclase are always lower than those of the Rietveld mode. The Rietveld method determines, as periclase, FeO and CaO amounts that occur in solid solution in periclase.  MAGNORM calculates these CaO amounts entirely as lime (if CaO is in access) or as another phases if there is sufficient SiO2 present.  The sums periclase + lime as determined by the mode, and periclase + lime as calculated by the norm should always compare very well;

* MAGNORM, in its present form, does not calculate tricalcium silicate as a separate phase. Therefore, the dicalcium silicate amount is always higher than the mode value.  This occurs because the normative dicalcium silicate value, incorporates tricalcium silicate by default.  When the mode values for dicalcium silicate and tricalcium silicate are added, the sum compares favourably with the dicalcium silicate norm value.

The mode and norm values for zirconia doped samples compare favourably. However, the two chromium doped test samples differ in their composition and show discrepancies between the two methods.  Additional test samples are needed in order to develop a correct procedure.

The mode and norm values of the nine samples that contain only high-melting-point phases compare favourably. The periclase + lime of the mode should be compared with periclase + lime of the norm, and the dicalcium silicate and tricalcium silicate of the mode should be compared with the dicalcium silicate of the norm.

Samples 2, 7 and 21 that contain merwinite compare favourably. However, the mode and norm results of the samples 20 and 22 differ in the merwinite content.

Only two samples occur in the group of samples containing merwinite and monticellite. Rietveld analysis found that both merwinite and monticellite were present in samples 13 and 19.  It is conceivable that the two phases are decomposition products of bredigite.  In both cases the norm calculates monticellite only.

Only the mode and norm results of bredingite-containing sample 17 are compatible.  Bredigite decomposes above 1375oC to dicalcium silicate and merwinite.  Therefore, at least theoretically, bredigite should not exist at temperatures used for refractory production.  The reason that bredigite can exist in undoped or zirconia doped magnesia refractories is not known.

Of the remaining samples with monticellite, the mode and norm results of sample 1 compare favourably.  The norm value for monticellite is lower because of a higher dicalcium silicate content.  The mode and norm results of  sample 29, do not compare favourably.

The only sample that contains akermanite(C2MS2) compares favourably, but MAGNORM does not calculate akermanite.  Akermanite accounts for only 0.10 wt.%, an amount that could be questioned.

Conclusions

MAGNORM calculates normative phase compositions of magnesia refractories, from their bulk chemical analyses.  Its advantages are the speed that results can be produced from predetermined chemical analysis, the low cost to produce them and consistency.  The same rules and assumptions apply to all calculations, allowing more meaningful comparison between samples.

The program, in its present form, has limitations, but improvements are not yet possible due to lack of test samples. For example MAGNORM:

* Does not differentiate between the dicalcium silicate and tricalcium silicate phases;

* Cannot differentiate between polymorphs (such as the dicalcium silicate phases that are all presented as "dicalcium silicate", and the silica phases that are all presented as "silica");

* Calculates only one hydrated compound (brucite), which is by far the most abundant of the possible phases;

* Cannot differentiate between CaO that exists as lime and CaO that exists in solid solution with MgO in periclase (excess CaO is presented as lime); * Presents the unused silica as excess silica, although magnesia refractories are made well above the melting point of silica.

The differences between mode and norm values noticed in some samples should not be interpreted as a failure of the norm to calculate the normative phases correctly.  A direct comparison of the two methods is not appropriate, because the accuracy of the XRD modes obtained for magnesia refractories using the Rietveld method has not yet been fully tested on these systems, and the norm calculates a hypothetical composition, that is unlikely to match the mode.  It should be accepted that each method has some advantages not available in the other.

Copies of the latest executable version of MAGNORM are available from the author on request.

Acknowledgments

The author would like to thank Mr. R.C.A. Flann (Project Manager, MgO refractories) for information, Dr. R.J. Hill for providing the X-ray model

analyses, and Mr B.W. Wilson for the XRF analyses. Further, the author wishes to thank  Dr. R.J. Hill, Dr. E.R. Segnit, Dr. W.G. Mumme, Dr. S. Fletcher and Dr. G.M Lukaszewski and Mr. R.C.A. Flann for their critical review of the manuscript.

References

1R.J.Hill. "Expanded use of the Rietveld method in studies of phase abundance in multiphase mixtures" Powder Diffraction, 6, No. 2, pp. 74-77 (1991).

2R.J.Hill "The background in X-ray powder diffractograms: A case study of Rietveld analysis of minor phases using Ni-filtered and graphite-monochromated radiation" Powder Diffraction, 7, No. 2, pp. 63-71 (1992).

3R.J.Hill, G.Tsambourakis, and I.C.Madsen. "Improved petrological modal analyses from X-ray powder diffraction data by use of the Rietveld method. I. Selected igneous, volcanic and metamorphic rocks" J. of Petrol. 34, part 5, pp. 867-900(1993).

4R.H.Bogue. "Calculation of the compounds in Portland cement. Ind. Eng. Chem., Anal. Ed., 1, No.4, pp. 192-197 (1927).

5C.M.Midgley "The crystal structure of b dicalcium silicate". Acta Cryst. 5, pp. 307-312(1952).

MAGNORM Calculations

Calcium to silica ratio (CSR) CSR=CaO:SiO2

The CaO to SiO2 ratio is considered to be an important parameter.  It is assumed that when the CaO/SiO2 ratio is higher than 2, high melting point compounds such as dicalcium silicate (C2S) and tricalcium silicate (C3S) are formed; however, when the ratio is lower than 2, then undesirable phases such as monticellite, merwinite and bredigite may form.   CSR=CaO/SiO2

Iron to calcium ratio (ICR)ICR=Fe2O3:CaO

The Fe2O3 to CaO ratio is important and can be successfully used to predict the refractory qualities of magnesite.  High ratios favour the presence of one or more of the undesirable phases monticellite merwinite and bredigite.  Small Fe2O3 amounts are negligible because of the iron's ability to enter into solid solution in the periclase as FeO at high temperatures.  Ideally, the Fe2O3 to CaO ratio should be below 0.1.  ICR=Fe2O3/CaO

Brucite MgO.H2O: The H2O amount present, combined with MgO is calculated as brucite (Bru).  One wt.% H2O plus 2.237 wt.% MgO form 3.237 wt.% Mg(OH)2.

A=2.237*H2O+.  Bru=H2O++A;  MgO=MgO-A.

Chromite (Cm) FeO.Cr2O3: The Cr2O3 amount present, combined with FeO is calculated as chromite (Cm).  One wt.% Cr2O3 plus 0.473 wt.% FeO form 1.473 wt.% FeCr2O4.  The FeO amount required is the converted to Fe2O3 (FeO*1.1113) before subtraction from the Fe2O3 content.

A=0.473*Cr2O3.  Cm=Cr2O3+A;  Fe2O3=Fe2O3-(1.1113*A).

Calcium zirconate (Cz) CaO.ZrO2: The ZrO2 content combined with CaO is calculated as calcium zirconate (Cz).  One wt.% ZrO2 plus 0.455 wt.% CaO form 1.455 wt.% CaZrO3.  =0.455*ZrO2.  Cz=ZrO2+A;  CaO=CaO-A.

Set: SiO2=SiO2+Al2O3; MgO=MgO+MnO+Fe2O3; V1=SiO2; V2=MgO; V3=CaO.

Special instructions:

If Cz>0 goto bredigite

If Cm>0 goto monticellite

If ICR³0.45 & CSR>4, goto merwinite

If ICR³0.45 & CSR>1.0 but CSR<4.0, goto bredigite

If ICR³0.45 & CSR£1.0, goto monticellite

If ICR>0.3 but ICR£0.45 & CSR<2.0, goto monticellite

If ICR>0.1 but ICR<0.3 & CSR£2.0, goto merwinite

If ICR>0.1 & CSR<1.0, goto monticellite

If none of the above applies continue with dicalcium silicate

Bredigite (C7MS4) 7CaO.MgO.4SiO2

If SiO2<CaO: One wt.% SiO2 plus 1.633 wt.% CaO plus 0.168 wt.% MgO form 2.801 wt.% C7MS4.   A=0.168*SiO2; B=1.633*SiO2. C7MS4=SiO2+A+B.

MgO=MgO-A; CaO=CaO-B; and SiO2=0.

If CaO<0 than; C7MS4=0; CaO=V3; MgO=V2; and SiO2=V1.

Goto monticellite.  If CaO³0, goto periclase.

If SiO2>CaO: One wt.% CaO plus 0.612 wt.% SiO2 plus 0.103 wt.% MgO form 1.715 wt.% C7MS4.  A=0.103*CaO; B=0.612*CaO. C7MS4=CaO+A+B.

MgO=MgO-A; SiO2=SiO2-B; and CaO=0.  Goto periclase.

A. LOOP: LOOP=LOOP+1.  Set: SiO2=Value A; MgO=Value B; CaO=Value C.

Dicalcium silicate (C2S) 2CaO.SiO2

If SiO2<CaO: One wt.% SiO2 plus 1.866 wt.% CaO form 2.866 wt.% C2S.

A=1.866*SiO2.  C2S=SiO2+A; CaO=CaO-A; SiO2=0.

If (CaO-A)>0, goto periclase.

If (CaO-A)<0, than: A=CaO/1.866; B=SiO2-A; and C=1.866*B.

C2S=B+C; CaO=CaO-C; SiO2=SiO2-B.  Goto monticellite.

If SiO2>CaO: One wt.% CaO plus 0.536 wt.% SiO2 form 1.536 wt.% C2S.

A=0.536*CaO.  C2S=CaO+A.  SiO2=SiO2-A; CaO=0.

If SiO2>0 and LOOP=0, set: C2S=0; CaO=V3; and SiO2=V1.

If LOOP>0, than CaO=A1 (see LOOP).

If (SiO2-A)>0, goto monticellite.

If (SiO2-A)<0, than: A=SiO2/0.536; B=CaO-A.

C2S=B+C; C=0.536*B; CaO=CaO-B; SiO2=SiO2-C.

Monticellite (CMS) CaO.MgO.SiO2

If SiO2<CaO: One wt.% SiO2 + 0.933 wt.% CaO + 0.671 wt.% MgO form 2.604 wt.% CMS.   A=0.933*SiO2; B=0.671*SiO2. CMS=SiO2+A+B.

CaO=CaO-A; MgO=MgO-B; and SiO2=0. If CaO>0 goto periclase.

If (CaO-A)<0, than: A=CaO/0.933; B=SiO2-A; C=0.933*B; and D=0.671*B.

CMS=B+C+D; SiO2=SiO2-A; CaO=CaO-C; and MgO=MgO-D.

LOOP: If LOOP>1, goto merwinite. If SiO2>0, set: DCS=0 and CMS=0.   A1=(SiO2/1.071)+((SiO2/1.071)*0.755).

Set: A=V1-SiO2; B=V2; C=V3-A1.  Goto LOOP

If SiO2>CaO: One wt.% CaO plus 1.071 wt.% SiO2 plus 0.719 wt.% MgO form 2.79 wt.% CMS.  A=1.071*CaO; B=0.719*CaO.  CMS=CaO+A+B.

SiO2=SiO2-A; MgO=MgO-B; and CaO=0.

Repeat LOOP. If (SiO2-A)<0 than: A=SiO2/1.071; B=CaO-A; C=1.071*B; and D=0.719*B.  CMS=B+C+D.

SiO2=SiO2-A; CaO=CaO-C; and MgO=MgO-D.

If SiO2=0 or CaO=0 goto periclase (6.5.1).  Repeat LOOP.

Merwinite (C3MS2)

If SiO2<CaO: One wt.% SiO2 plus 1.4 wt.% CaO plus 0.335 wt.% MgO form 2.735 wt.% C3MS2.  A=1.4*SiO2; B=0.335*SiO2. C3MS2=SiO2+A+B.

CaO=CaO-A; MgO=MgO-B; and SiO2=0. If CaO>0, goto periclase (6.5.1.).

If CaO<0, than: C3MS2=0; CaO=CaO+A; MgO=MgO+B; SiO2=B/0.355.  Goto monticellite (5.4.3.).

If SiO2>CaO: One wt.% CaO plus 0.714 wt.% SiO2 plus 0.239 wt.% MgO form 1.953 wt.% C3MS2.   A=0.714*CaO; B=0.239*CaO.  C3MS2=CaO+A+B.

SiO2=SiO2-A; MgO=MgO-B; and CaO=0.

If SiO2>0 than: C3MS2=0; SiO2=SiO2+A; MgO=MgO+B; and CaO=B/0.239.  Goto monticellite (5.4.3.)

The phases: Periclase, lime and excess silica

Periclase (Per) MgO: The remaining MgO is presented as periclase (Per).  Per=MgO

Lime (Lm) CaO: The remaining CaO that is the CaO not used in the calculations is presented as lime (Lm).  Lm=CaO.

Excess Silica (Si) SiO2: If for any reason, there is still silica left, then the remaining SiO2 is presented as Excess silica.  Si=SiO2.

GT:RSP:09.11.94:MAGNEW1.DOC:DSK:B:31