CALCULATION PROCEDURE

5.1.  Parameters.

5.1.1. Calcium to silica ratio (CSR) CSR=CaO:SiO2.

The CaO to SiO2 ratio is considered to be an important parameter because it reveals the refractory qualities of magnesite.  It is assumed that when the CaO/SiO2 ratio is higher than 2, high melting point compounds such as dicalcium silicate (C2S) and tricalcium silicate (C3S) are formed; however, when the ratio is lower than 2, then undesirable phases such as monticellite, merwinite and bredigite may form.

CSR = CaO/SiO2

5.1.2. Iron to calcium ratio (ICR)ICR=Fe2O3:CaO.

The Fe2O3 to CaO ratio is also important and can be successfully used to predict the refractory qualities of magnesite.  High ratios favour the presence of one or more of the undesirable phases monticellite merwinite and bredigite.  Small Fe2O3 amounts are negligible because of the irons ability to enter into solid solution in the periclase as FeO at high temperatures.  Ideally, the Fe2O3 to CaO ratio should be below 0.1.

ICR = Fe2O3/CaO

5.2. The phases: Brucite, chromite and calcium zirconate.

5.2.1. Brucite (Bru). MgO.H2O.

The H2O amount present, combined with MgO is calculated as brucite (Bru).  One wt.% H2O plus 2.237 wt.% MgO form 3.237 wt.% Mg(OH)2.

MgO    40.3044

---- = ------- = 2.237 (wt.%) MgO.

H2O+    18.015

A = 2.237 * H2O+;	Bru = H2O+ + A;	MgO = MgO - A

5.2.2. Chromite (Cm) FeO.Cr2O3.

The Cr2O3 amount present, combined with FeO is calculated as chromite (Cm).  One wt.% Cr2O3 plus 0.473 wt.% FeO form 1.473 wt.% FeCr2O4.  The FeO amount required is the converted to Fe2O3 (FeO*1.1113) before subtraction from the Fe2O3 content.

FeO      71.8464

----- = -------- = 0.473 (wt.%) FeO;

Cr2O3   151.9904

A = 0.473 * Cr2O3.	Cm = Cr2O3 + A.	Fe2O3 = Fe2O3 - (1.111*A)

5.2.3. Calcium zirconate (Cz) CaO.ZrO2.

The ZrO2 content combined with CaO is calculated as calcium zirconate (Cz).  One wt.% ZrO2 oplus 0.455 wt.% CaO form 1.455 wt.% CaZrO3.

CaO     56.0774

---- = -------- = 0.455 wt.% CaO.

ZrO2   123.2228

A = 0.455 * ZrO2.	Cz = ZrO2 + A;	CaO = CaO - A

After the above calculations set:

SiO2 = SiO2 + Al2O3;	MgO = MgO + MnO + Fe2O3.

V1 = SiO2;	V2 = MgO;		V3 = CaO.

5.3. Special instructions: At this stage the following conditions are introduced which are based on observations on refractories.

5.3.1. If Cz>0 goto bredigite(5.4.1.)

5.3.2. If Cm>0 goto monticellite (5.4.3.).

5.3.3. If ICR is greater or equal 0.45 and CSR>4, goto merwinite (5.4.4.).

5.3.4. If ICR is greater or equal 0.45 and CSR is greater than 1.0 but less than 4.0, goto bredigite (5.4.1.).

5.3.5. If ICR is greater or equal 0.45 and CSR is less or equal 1.0, goto monticellite (5.4.3.).

5.3.6. If ICR is greater than 0.3 but lower or equal 0.45 and CSR<2.0, goto monticellite (5.4.3.).

5.3.7. If ICR is greater than 0.1 but less than 0.3 and CSR is less or equal 2.0, goto merwinite (5.4.4.).

5.3.8. If ICR>0.1 and CSR<1.0, goto monticellite (5.4.3.).

If none of the above rules applies continue with dicalcium silicate (5.4.2.).

5.4. The phases: Bredigite, dicalcium silicate, monticellite and merwinite.

5.4.1. Bredigite (C7MS4) 7CaO.MgO.4SiO2.

5.4.1.1. If SiO2<CaO.

One wt.% SiO2 plus 1.633 wt.% CaO plus 0.168 wt.% MgO form 2.801 wt.% C7MS4.

MgO      40.3044

----- = -------- = 0.168 wt.% MgO;	A = 0.168 * SiO2

4SiO2   240.3372

7CaO    392.5418

----- = -------- = 1.633 wt.% CaO;	B = 1.633 * SiO2

4SiO2   240.3372

C7MS4 = SiO2 + A + B.

MgO = MgO - A;		CaO = CaO - B;		SiO2 = 0.

If CaO<0, than C7MS4 = 0.	CaO = V3;	MgO = V2;		SiO2 = V1.

Goto with monticellite (5.4.3)

If CaO is greater or equal zero, goto periclase (6.5.1.).

5.4.1.2. If SiO2>CaO.

One wt.% CaO plus 0.612 wt.% SiO2 plus 0.103 wt.% MgO form 1.715 wt.% C7MS4.

MgO     40.3044

---- = -------- = 0.103 (wt.%) MgO;	A = 0.103 * CaO.

7CaO   392.5418

4SiO2   240.3372

----- = -------- = 0.612 (wt.%) SiO2;	B = 0.612 * CaO.

7CaO    392.5418

C7MS4 = CaO + A + B;	MgO = MgO - A;		SiO2 = SiO2 - B;

CaO = 0.		Goto periclase (6.5.1.).

5.4.2.A. LOOP

LOOP = LOOP + 1.

Set: SiO2 = Value A;	MgO = Value B;		CaO = Value C.

5.4.2. Dicalcium silicate (C2S) 2CaO.SiO2.

5.4.2.1. If SiO2<CaO.

One wt.% SiO2 plus 1.866 wt.% CaO form 2.866 wt.% C2S.

2CaO   112.1548

---- = -------- = 1.866 wt.% CaO;

SiO2    60.0843

A = 1.866 * SiO2;	C2S = SiO2 + A;	CaO = CaO - A;	SiO2 = 0.

If (CaO - A)>0, goto periclase (6.5.1.).

If (CaO - A)<0, set: A = CaO/1.866; B = SiO2-A; C = 1.866*B.

C2S = B + C;	CaO = CaO - C;	SiO2 = SiO2 - B.

Goto monticellite (5.4.3.)

5.4.2.2. If SiO2>CaO.

One wt.% CaO + 0.536 wt.% SiO2 form 1.536 wt.% C2S.

SiO2    60.0843

---- = -------- = 0.536 wt.% SiO2;

2CaO   112.1548

A = 0.536 * CaO;	C2S = CaO + A;	SiO2 = SiO2 - A;	CaO = 0.

If SiO2>0 and LOOP=0, set: C2S = 0;	CaO = V3;		SiO2 = V1.

If LOOP>0, set CaO = A1 (see LOOP(5.4.3.2.)).

If (SiO2 - A)>0, goto monticellite (5.4.3.).

If (SiO2 - A)<0, set:

A = SiO2/0.536;	B = CaO - A;	C = 0.536 * B.

C2S = B + C;	CaO = CaO - B;		SiO2 = SiO2 - C.

5.4.3. Monticellite (CMS) CaO.MgO.SiO2.

5.4.3.1. If SiO2<CaO.

One wt.% SiO2 plus 0.933 wt.% CaO plus 0.671 wt.% MgO form 2.604 wt.% CMS.

CaO    56.0774

---- = ------- = 0.933 wt.% CaO;	A = 0.933 * SiO2.

SiO2   60.0843

MgO    40.3044

---- = ------- = 0.671 wt.% MgO;	B = 0.671 * SiO2.

SiO2   60.0843

CMS = SiO2 + A + B;	CaO = CaO - A;	MgO = MgO - B;	SiO2 = 0.

If CaO>0, goto periclase (6.5.1.).

If (CaO - A)<0, set:

A = CaO/0.933;	B = SiO2 - A;	C = 0.933 * B;	D = 0.671 * B.

CMS = B + C + D;	SiO2 = SiO2 - A;	CaO = CaO - C;

MgO = MgO - D.

5.4.3.2. LOOP:

If LOOP>1, goto merwinite (5.4.4.).

If SiO2>0, set: DCS = 0;	CMS = 0.

A1 = (SiO2/1.071) + ((SiO2/1.071) * 0.755).

Set: A = V1 - SiO2;	B = V2;	C = V3 - A1.  Goto LOOP (5.4.2.A.)

5.4.3.3. If SiO2>CaO.

One wt.% CaO plus 1.071 wt.% SiO2 plus 0.719 wt.% MgO form 2.79 wt.% CMS.

SiO2   60.0843

---- = ------- = 1.071 wt.% SiO2;	A = 1.071 * CaO.

CaO    56.0774

MgO   40.3044

--- = ------- = 0.719 wt.% MgO;		B = 0.719 * CaO.

CaO   56.0774

CMS = CaO + A + B;	SiO2 = SiO2 - A;	MgO = MgO - B;

CaO = 0.

Repeat LOOP (5.4.3.2.).

If (SiO2 - A)<0, set:

A = SiO2/1.071;	B = CaO - A;	C = 1.071 * B;	D = 0.719 * B.

CMS = B + C + D;	SiO2 = SiO2 - A;	CaO = CaO - C;

MgO = MgO - D.

If SiO2=0 or CaO=0 goto periclase (6.5.1).

Repeat LOOP (5.4.3.2.).

5.4.4. Merwinite (C3MS2).

5.4.4.1. If SiO2<CaO.

One wt.% SiO2 plus 1.4 wt.% CaO plus 0.335 wt.% MgO form 2.735 wt.% C3MS2.

3CaO   168.2322

----- = -------- = 1.4 wt.% CaO;	A = 1.4 * SiO2.

2SiO2   120.1686

MgO    40.3044

----- = -------- = 0.335 wt.% MgO;	B = 0.335 * SiO2.

2SiO2   120.1686

C3MS2 = SiO2 + A + B;	CaO = CaO - A;	MgO = MgO - B;

SiO2 = 0.

If CaO>0, goto periclase (6.5.1.).

If CaO<0, set:	C3MS2 = 0;	CaO = CaO + A;	MgO = MgO + B;

SiO2 = B/0.355.  Go to monticellite (5.4.3.).

5.4.4.2. If SiO2>CaO.

One wt.% CaO plus 0.714 wt.% SiO2 plus 0.239 wt.% MgO = 1.953 wt.% C3MS2.

2SiO2   120.1686

----- = -------- = 0.714 wt.% SiO2;	A=0.714*CaO.

3CaO   168.2322

MgO     40.3044

----- = -------- = 0.239 wt.% MgO;	B=0.239*CaO.

3CaO   168.2322

C3MS2 = CaO + A + B;	SiO2 = SiO2 - A;	MgO = MgO - B;

CaO = 0.

If SiO2>0, set:

C3MS2 = 0;	SiO2 = SiO2 + A;	MgO = MgO + B;	CaO = B/0.239. Goto monticellite (5.4.3.)

6.5. The phases: Periclase, lime, excess silica.

6.5.1. Periclase (Per) MgO.

The remaining MgO is presented as periclase (Per).

Per = MgO

6.5.2. Lime (Lm) CaO.

The remaining CaO that is the CaO not used in the calculations is presented as lime (Lm).

Lm = CaO.

6.5.3. Excess Silica (Si) SiO2.

If for any reason, there is still silica left, then the remaining SiO2 is presented as Excess silica.

Si = SiO2.

GT:RSP:21.06.94:MGNORM.DOC:DSK:B:27